Antiferromagnetic Ordering Enhanced Magnetic Damping in Mn2Au/CoFeB Bilayers

Donghang Xie1,2 , Haozhe Wang1,3 , Zhe Zhang1,2 , Zishuang Li1,3 , Jiahua Lu1,2 , Ronghua Liu1,3,a) , Jun Du1,3, Bo Liu1,2 , Yu Yan1,2 , Liang He1,2 , Jing Wu4 , Rong Zhang2 , Bo Liu5, Tiejun Zhou5, Yongbing Xu1,2,4,a) , Xuezhong Ruan1,2,a)

AFFLIATIONS

1 State Key Laboratory of Spintronics, Nanjing University, Suzhou, 215163, China

2 Jiangsu Provincial Key Laboratory of Advanced Photonic and Electronic Materials, School of Electronic Science and Engineering, Nanjing University, Nanjing 210093, China

3 School of Physics, Nanjing University, Nanjing 210093, China

4 York-Nanjing Joint Center (YNJC) for Spintronics and Nano Engineering, Department of Electronics and Physics, The University of York, York YO10 5DD, UK

5 State Key Laboratory for Spintronic Devices and Technologies, Hangzhou 311305, China

a) Authors to whom correspondence should be addressed: rhliu@nju.edu.cn, ybxu@nju.edu, and xzruan@nju.edu.cn

ABSTRACT

Antiferromagnets (AFMs) hold significant potential for spintronic devices owing to their insensitivity to external magnetic fields and the absence of stray fields. Beyond these inherent advantages, an AFM can manipulate the magnetic dynamics of a ferromagnet (FM) layer in AFM/FM bilayers, whereas the mechanism of such manipulation remains controversial. Here, we investigate the magnetic dynamics of AFM/FM Mn2Au/CoFeB bilayers via Ferromagnetic Resonance (FMR). It is found that the Néel temperature of 2-nm-thick Mn2Au is as low as 40 K, in sharp contrast to that of bulk Mn2Au, which exceeds 1000 K. In the Mn2Au(2 nm)/CoFeB(4 nm) bilayer, the magnetic damping α of the CoFeB layer increases from 0.013 to 0.047 as temperature decreases from 160 K to 10 K, accompanied by a synchronous increase in the exchange coupling field Hrot. Such an increase of α is attributed to the enhanced spin angular momentum transfer from CoFeB to Mn2Au, mediated through AFM-FM exchange coupling between Mn2Au and CoFeB, which is enhanced by the Mn2Au antiferromagnetic ordering as the temperature decreases. Our study provides deeper insights into AFM/FM dynamics and spintronic storage technology.

In recent years, Magnetic Random Access Memory (MRAM) has attracted increasing attention in the field of modern storage technology due to its low power consumption, high speed, and non-volatility, positioning it as a promising alternative to conventional storage devices.1,2 The operation of MRAM relies on the switching of magnetic moments between the “0” and “1” states in magnetic tunnel junctions (MTJs) such as CoFeB/MgO/CoFeB.3,4 Therefore, understanding and controlling the magnetization dynamics of these ferromagnets (FMs) has become a central focus in both fundamental research and industrial applications. In ferromagnetic dynamics, the magnetic damping and the anisotropy field are two key parameters that determine the critical switching current density and the stable orientation of magnetic moments, respectively.5 Consequently, exploring effective approaches to modulate these parameters is essential for the development of magnetic storage technology.

Antiferromagnetic (AFM) materials, insensitive to external magnetic fields and free of stray fields,6–10 hold significant promise for next-generation magnetic storage devices. Beyond these intrinsic features, the antiferromagnet/ferromagnet (AFM/FM) exchange-coupled systems exhibit intriguing properties, including improved thermal stability,11–13 achievement of perpendicular magnetic anisotropy (PMA) in the FM layer,14–18 and field-free THz emission.19 Moreover, the magnetic dynamics of the FM layer can be significantly modulated by the adjacent AFM. Fan et al. studied the magnetic dynamics in CoO/Fe and attributed the enhanced damping to exchange coupling.20 Zhang et al. correlated the increased damping in FeGa/IrMn with the ultrafast demagnetization rates and attributed it to the competition between FM and AFM spin pumping.21 Frangou et al. emphasized spin pumping as the dominant mechanism responsible for the magnetic dynamics in AFM/FM bilayers.22 Liu et al. proposed that the interfacial exchange spring effect is responsible for the damping modulation in IrMn/CoFe.23 Despite these reports, no consensus exists on the mechanism by which the AFM manipulates the magnetic dynamics of FM. These aspects highlight the need for further investigation into the magnetic dynamics of AFM/FM heterostructures.

Furthermore, investigations on the modulation of magnetic dynamics in FM by an adjacent AFM layer have motivated the exploration of novel AFM materials. As a member of the collinear AFM family, Mn2Au exhibits a robust AFM-FM exchange coupling effect24,25 and strong sublattice magnetization (~4μB).26 Its Néel temperature (TN) exceeds 1000 K, endowing Mn2Au with excellent thermal stability for high-temperature spintronic applications.26,27 Although theory predicts that the TN of an AFM film may be suppressed when its thickness is reduced to a few nanometers,28,29 it remains unclear whether the AFM order in Mn₂Au persists at such ultrathin thicknesses. If it does, how would an ultrathin Mn₂Au layer affect the magnetic dynamics of an adjacent FM layer in the Mn2Au/FM bilayers? Therefore, in this work, we employ temperature-dependent ferromagnetic resonance (FMR) to systematically investigate the magnetic dynamics of Mn2Au/CoFeB bilayers with nanometer-thick Mn2Au layers. Superconducting Quantum Interference Device (SQUID) measurements confirm the AFM order in Mn2Au with a thickness down to 2 nm. Temperature-dependent FMR measurements on Mn2Au(2 nm)/CoFeB bilayer show that magnetic damping (α) remains nearly unchanged and the exchange coupling field (Hrot) is absent above 160 K, while both α and Hrot increase significantly as temperature decreases below 160 K, exhibiting a synchronous trend. In contrast, for the reference sample CoFeB, the α remains nearly unchanged and Hrot is absent from room temperature to 10 K. The damping increase is eliminated by inserting an Al interlayer between Mn2Au and CoFeB layers, ruling out the spin pumping effect, and indicating that the enhanced damping is attributed to the enhanced spin angular momentum transfer mediated by the AFM-FM exchange coupling, which is strengthened by the Mn2Au antiferromagnetic ordering as the temperature decreases. Our study provides deeper insight into the mechanism of the AFM-FM exchange-coupled systems and their potential in magnetic storage applications.

The following structures were deposited on Si substrates by Magnetron Sputtering: Si/MgO(3)/Mn₂Au(2)/Co40Fe40B20(4)/Al(3) (denoted as Mn2Au(2)/CoFeB), Si/MgO(3)/Mn₂Au(4)/Co40Fe40B20(4)/Al(3) (denoted as Mn2Au(4)/CoFeB), Si/MgO(3)/Mn₂Au(2)/Al(1.5)/Co40Fe40B20(4)/Al(3) (denoted as Mn2Au(2)/Al/CoFeB), and the reference sample Si/MgO(3)/Co40Fe40B20(4)/Al(3) (denoted as CoFeB). The numbers in the parentheses are the layer thickness in nanometers. The MgO seed layer was deposited by RF sputtering to optimize the growth of Mn2Au and CoFeB. All other layers were deposited by DC sputtering. Mn2Au was sputtered from an alloy target (atomic ratio: Mn: Au=2:1). The base pressure was better than 9×10⁻⁸ Torr, and the working argon pressure was set at 7 mTorr. The Al capping layer prevented oxidation. Static magnetic properties were characterized using a Superconducting Quantum Interference Device (SQUID). The magnetic dynamics were studied by Ferromagnetic Resonance (FMR). In the FMR setup shown in Fig. 2(a), the sample was placed face-down on a coplanar waveguide (CPW), ensuring optimal contact with the radio-frequency field Hrf, generated by an rf-current Irf applied through the CPW at various frequencies. The FMR measurements were conducted in a vacuum (better than 1×10-5 Pa) from room temperature (RT) to 10 K. A second coil was installed in the magnet, and a lock-in amplifier (LIA) was used to improve the signal quality.

FIG. 1. (a) In-plane magnetic hysteresis loop of Mn2Au(2)/CoFeB at RT. The saturation magnetization MS is 1140 emu/cc. (b) Temperature-dependent exchange bias field HEB and increment of coercivity ΔHC.

The magnetic hysteresis loop of Mn2Au(2)/CoFeB at RT is presented in Fig. 1(a). The saturation magnetization MS is 1140 emu/cc, consistent with reported values for CoFeB.30–33 To verify AFM order, field-cooled magnetic hysteresis loops were measured using SQUID (see supplementary material, Fig. S1). The sample was cooled from RT to 4 K under an in-plane field of 5 kOe. Exchange bias field HEB and increment of coercivity ΔHC (ΔHC=HC-HC(RT)) were observed at 4 K, confirming the presence of macroscopic AFM order in the 2 nm Mn2Au layer at low temperature. As the temperature increases, HEB disappears at ~10 K, and ΔHC disappears at ~40 K (see supplementary material, Fig. S1 and Fig. 1(b)). In contrast, the coercivity of a stand-alone CoFeB layer remains unchanged between RT and 5 K.4 As reported by Lenz et al., the enhanced coercivity in AFM/FM bilayer arises from AFM order, and the temperature at which ΔHC disappears upon warming is regarded as the Néel temperature TN.18,34 Accordingly, we conclude that the TN of 2 nm Mn2Au is approximately 40 K.

FIG. 2. (a) Schematic illustration of the FMR setup. (b) FMR signals at 11 GHz Hrf for Mn2Au(2)/CoFeB at 280K, 240K, 140K, 90K and 40 K. For better comparison, the 140 K signal is amplified by 1.5 times, while the 90 K and 40 K signals are amplified by 5 times. The solid lines are the fitting results of Equation (1). (c) FMR dispersion relation (f-Hres). (d) Frequency-dependent FMR linewidth (ΔHPP-f). The linewidths at 40 K and 90 K are shifted downward by 0.05 kOe for a better comparison. The solid lines are fits to Equation (2) and (3), respectively.

Dynamic magnetic properties were characterized via ferromagnetic resonance (FMR). Fig. 2(a) presents the schematic of the FMR setup. A radio-frequency magnetic field (Hrf) with variable frequency (f) was applied along the x-axis, while a static magnetic field (H) was applied along the y-axis. By sweeping H, the magnetization of the FM layer resonates when H matches the resonant field (Hres) for a given frequency of Hrf, leading to absorption of the rf field, detected as the FMR signal. Fig. 2(b) presents the experimental FMR signals from Mn2Au(2)/CoFeB as a function of the magnetic field, measured at a fixed Hrf frequency of 11 GHz across various temperatures. These signals were fitted by the derivative of a Lorentzian function:35

y=y0-S2∙ΔH2∙H-HresH-Hres2+ΔH22+AΔH2-H-Hres2∙ΔHH-Hres2+ΔH22#1

In this equation, ΔH is half of the peak-to-peak linewidth ΔHPP and Hres is the resonant field. As shown in Fig. 2(b), two prominent features emerge in the FMR signal as the temperature decreases. First, the resonance field Hres systematically shifts toward zero. Second, the peak-to-peak linewidth ΔHPP of the FMR signals broadens significantly. Here, the shift of Hres suggests an “internal” magnetic field, which is built up inside the sample and effectively compensates the applied external field. Furthermore, such a shift is isotropic in the film plane, as indicated by the isotropic in-plane angular-dependence of Hres shown in the supplementary material Fig. S2. Unlike the unidirectional shift from pinned uncompensated AFM spins-induced exchange bias,36 the observed isotropic shift originates from the rotatable anisotropic field (Hrot) arising from interfacial exchange coupling between unpinned (rotatable) uncompensated AFM spins and FM spins.37–39 Therefore, we also refer to Hrot as the “exchange coupling field” in this work. The dispersion relation (Hres as a function of resonant frequency f) is plotted in Fig. 2(c) and is well described by the following equation:40

f=γ(Hres+Hrot+HEB)Hres+Hrot+HEB+4πMeff#2

where γ, 4πMeff, Hrot, and HEB are the gyromagnetic ratio, effective demagnetization field, rotatable anisotropy field, and exchange bias field, respectively. We used 2.8 GHz/kOe for γ in our fitting.41 The value of HEB was obtained from the shift of the magnetic hysteresis loop measured by SQUID (see Fig. 1(b)). Here, 4πMeff=4πMS-2K⊥MS, where K⊥ is the perpendicular anisotropy constant. For Mn2Au(2)/CoFeB, 4πMeff at RT was determined to be 14.5 kOe from the saturation field of the out-of-plane hysteresis loop (see supplementary material, Fig. S3) and fitting dispersion relation at RT. This value is close to the demagnetization field 4πMS=14.3 kOe. The close agreement between 4πMeff and 4πMS indicates that K⊥ is negligible. As temperature decreases, the increase in MS renders the term 2K⊥MS even more negligible. Therefore, in our analysis, we approximated 4πMeff as 4πMS, with 4πMS obtained from the M-T curve measured by SQUID (see supplementary material, Fig. S4).

The extracted peak-to-peak linewidth ΔHPP as a function of f is shown in Fig. 2(d). The magnetic damping is obtained by fitting the data with the following equation:42

ΔHPP=ΔH0+23αγf#3

Here, ΔH0 denotes the inhomogeneous linewidth broadening and α is the effective magnetic damping. As shown in Fig. 3(a), the α of the reference sample CoFeB remains nearly invariant at ~0.011 from RT down to 10 K. This invariability is consistent with reported results.43 However, when the CoFeB layer is deposited on 2-nm-thick Mn2Au, the temperature dependence of α changes dramatically. From RT down to ~160 K, α of Mn2Au(2)/CoFeB remains nearly unchanged at about 0.013. As the temperature further decreases below 160 K, the magnetic damping increases pronouncedly, reaching 0.047 at 10 K. Meanwhile, Fig. 3(b) shows the temperature-dependence of the extracted rotatable anisotropic field Hrot. For the reference sample CoFeB, Hrot is nearly zero over the entire temperature range. Thus, Hrot of the reference sample CoFeB is negligible. In contrast, the Hrot of Mn2Au(2)/CoFeB remains near 0 kOe between 160 K and RT, and increases dramatically below about 160 K. This temperature dependence is analogous to that of α for Mn2Au(2)/CoFeB. The synchronous increase of α and Hrot with decreasing temperature indicates that they should share a common physical origin in the Mn2Au/CoFeB bilayer.

FIG. 3. (a) Temperature-dependent magnetic damping α of Mn2Au(2)/CoFeB, Mn2Au(2)/Al(1.5)/CoFeB and reference sample CoFeB. (b) Temperature-dependent rotatable anisotropic field Hrot of Mn2Au(2)/CoFeB and reference sample CoFeB. The dashed lines are the visual guides.

The temperature dependence of α and Hrot in the Mn2Au(2)/CoFeB bilayer contrasts markedly with that of the reference sample CoFeB. Two-magnon scattering (TMS)—a process in which a magnon with zero wave-vector (k=0) scatters into degenerate, nonuniform spin waves (k≠0) due to fluctuating exchange coupling and exchange bias at the interface21—has been widely studied in AFM/FM and heavy metal/FM bilayers. It is known that TMS can be suppressed by an externally applied field or exchange coupling field, leading to a reduction of damping.20,32 This feature contradicts our results in Fig. 3, where the α rises as Hrot increases in Mn2Au(2)/CoFeB. Thus, TMS is not the dominant mechanism in Mn2Au/CoFeB. The good linearity in the FMR linewidth vs. frequency curves in Fig. 2(d) and the polar-angle-dependent linewidth (see Supplemental Materials Fig.S5) further excludes TMS.44,45

The spin pumping effect (SPE) is known to modify damping in AFM/FM or heavy-metal/FM heterostructures by transporting electronic spin current.21,46,47 To investigate whether the enhanced damping below 160 K arises from spin pumping, we inserted a 1.5 nm Al interlayer between the Mn2Au and CoFeB layers. Aluminum, with weak spin-orbit coupling and long spin diffusion length, serves as an ideal spacer that maintains SPE while decoupling the magnetic layers.48 If SPE were the dominant mechanism, the damping should remain unaffected by inserting a thin Al layer. Fig. 3(a) compares the α of Mn2Au(2)/Al/CoFeB and Mn2Au(2)/CoFeB. Inserting Al interlayer reduces α below 160 K to about 0.012, a value identical to that of Mn₂Au(2)/CoFeB above 160 K. The elimination of damping increment by the Al interlayer indicates that the enhanced damping is caused not by SPE, but rather by an interaction requiring direct contact between Mn₂Au and CoFeB layers. Given that SQUID measurements demonstrate the emergence of AFM order in 2-nm-thick Mn2Au below 40 K and the synchronous increase of Hrot, we attribute the increase of α to the spin angular momentum transfer, mediated by exchange coupling between AFM Mn2Au and FM CoFeB. As the temperature decreases, the strengthened Mn2Au AFM order further enhances this exchange coupling and thus the spin angular momentum transfer, leading to the enhancement of α.

As the temperature decreases from RT to 160 K, the Mn2Au layer remains paramagnetic. The absence of AFM order precludes exchange coupling between Mn2Au and CoFeB, resulting in negligible Hrot acting on the CoFeB layer. Consequently, spin angular momentum transfer from CoFeB to Mn2Au is suppressed, leading to negligible damping variation.

As the temperature decreases from 160 K to TN (~40 K, as concluded from SQUID measurements), the emerging interfacial AFM-FM exchange coupling, established by short-range AFM order in Mn2Au, enables spin angular momentum transfer and dissipation from CoFeB to Mn2Au, thereby enhancing the damping. Key evidence supporting this mechanism is the synchronous increase in the exchange coupling field Hrot, a direct manifestation of interfacial exchange coupling between AFM spins in Mn2Au and FM spins in CoFeB.37,38,49 Here, SQUID probes macroscopic AFM order, whereas FMR probes microscopic one (see Supplemental Materials for discussion on static and dynamic measurements). Due to FMR's higher microscopic sensitivity over SQUID, we consider Hrot, not HEB or ΔHC, as the most accurate reflection of exchange coupling. Although macroscopic AFM order in Mn2Au only establishes below TN, the short-range AFM order well above TN has been widely reported,50–52 and these fluctuating AFM spins can generate Hrot by exchange coupling with FM.40,53,54 Meanwhile, this exchange coupling enables the precessing magnetization of CoFeB to exert a torque on Mn₂Au, thereby transferring the spin angular momentum to Mn₂Au.20,55 The transferred spin angular momentum is efficiently relaxed due to the strong spin-orbit coupling in Mn2Au, manifesting as spin angular momentum dissipation.56 Consequently, with decreasing temperature, the short-range AFM order of Mn2Au strengthens, enhancing the AFM-FM exchange coupling and facilitating spin angular momentum transfer and dissipation from CoFeB into Mn2Au, thus leading to the increase in α. Fig. 4 schematically illustrates this transfer and dissipation process. As the temperature decreases below 160 K, AFM order progressively establishes in the Mn2Au layer, thereby enhancing the AFM-FM exchange coupling between Mn2Au and CoFeB. These effects collectively strengthen Hrot and drive an efficient spin angular momentum transfer and dissipation, leading to the substantial enhancement of α.

Below TN, the establishment of macroscopic AFM order in Mn2Au further strengthens the exchange coupling, leading to further enhancement of both Hrot and α. The exchange coupling between the Mn₂Au AFM order and the CoFeB magnetization directly generates Hrot, and simultaneously facilitates spin angular momentum transfer and dissipation, thereby accounting for the observed increase of α. Several previous studies on AFM/FM bilayers have suggested that the AFM-FM exchange coupling is the possible mechanism behind magnetic damping,20,21,23,57,58 but the key physical parameters characterizing this coupling, such as the exchange coupling field Hrot, remain insufficiently explored. Our study not only quantitatively determines the value of the exchange coupling field, but also, more importantly, reveals a synchronous trend between magnetic damping and the AFM-FM exchange coupling field.

We further investigated the temperature-dependent α and Hrot in Mn2Au/CoFeB with 4-nm-thick Mn2Au layer (see supplementary material, Fig. S6). Mn2Au(4)/CoFeB exhibits a synchronized increase in Hrot and α as temperature decreases from RT to 100 K. This observation can be understood by the thickness-dependent TN in AFM materials. Previous studies have demonstrated that critical temperature (TN or TC) scales with film thickness.22,28,29,51,59,60 Ultrathin AFM films exhibit a suppressed TN, while TN of thicker films approaches the bulk value. Therefore, the increased Mn2Au thickness elevates TN toward the bulk value (>1000 K), causing the enhancement of α and Hrot to emerge synchronously at around RT in Mn2Au(4)/CoFeB. This feature contrasts sharply with that of Mn2Au(2)/CoFeB, where the damping enhancement only appears below 160 K. This explicit Mn2Au thickness dependence provides compelling evidence that the synchronized enhancement of Hrot and α is intrinsically linked to the AFM order of the Mn2Au layer.

FIG. 4. Schematic illustration of the physical mechanism of spin angular momentum transfer and dissipation in the Mn2Au(2)/CoFeB. Below 160 K, AFM order (represented by paired blue arrows in the Mn2Au layer) and AFM-FM exchange coupling (depicted as the spring between Mn2Au and CoFeB) are established and progressively enhanced with decreasing temperature. This leads to a synchronized increase of Hrot and efficient spin angular momentum transfer (illustrated by the gray span with the dashed red arrows moving from CoFeB into Mn2Au) and dissipation (illustrated by the randomly arranged dashed red arrows in Mn2Au), thereby enhancing the damping α.

In summary, we investigated the temperature-dependent magnetic dynamics of Mn2Au/CoFeB bilayers using FMR. For the Mn2Au(2 nm)/CoFeB bilayer, the magnetic damping α remains unchanged and the rotatable anisotropic field Hrot is negligible above 160 K. Below this temperature, both parameters increase dramatically and synchronously. The damping enhancement is attributed to spin angular momentum transfer and dissipation mediated by the exchange coupling between Mn2Au and CoFeB, which is enhanced by Mn2Au AFM ordering as temperature decreases. Analogous enhancement of damping is also observed in the Mn2Au(4 nm)/CoFeB bilayer near room temperature, conclusively confirming its dependence on the Mn2Au AFM ordering. These findings provide a deeper insight into magnetic dynamics in AFM/FM bilayers and have implications for the design of spintronic devices.

This work is supported by the National Key Research and Development Program of China (No. 2024YFA1408801), National Natural Science Foundation of China (Grant No. 62427901, 12574125, T2394473), and the Natural Science Foundation of Jiangsu Province of China (BK20211144).

SUPPLEMENTARY MATERIAL

See the supplementary material for additional information on magnetic hysteresis loops of field-cooled Mn2Au(2)/CoFeB samples, in-plane angular-dependent resonant field, out-of-plane magnetic hysteresis loop for Mn2Au(2)/CoFeB, M-T curve of Mn2Au(2)/CoFeB by SQUID, polar angle-dependent FMR linewidth, temperature-dependent magnetic damping and Hrot of Mn2Au(4)/CoFeB, discussion about the physical origin of Hrot, HEB, ΔHC, and difference between FMR and SQUID measurement, temperature-dependent inhomogeneous linewidth broadening and exchange coupling constant, temperature-dependent damping of Mn2Au(4)/CoFeB(3) by TR-MOKE measurement.

AUTHOR DECLARATIONS

Conflict of Interest

The authors have no conflicts to disclose.

Author Contributions

Donghang Xie: Conceptualization (equal); Data curation (lead); Formal analysis (equal); Investigation (equal); Methodology (equal); Software (equal); Validation (equal); Writing – original draft (lead); Writing – review & editing (equal). Haozhe Wang: Data curation (equal); Software (equal); Methodology (equal). Zhe Zhang: Data curation (equal). Zishuang Li: Data curation (equal). Jiahua Lu: Data curation (equal). Ronghua Liu: Data curation (equal); Formal analysis (equal); Funding acquisition (equal); Methodology (equal); Project administration (equal); Supervision (equal). Jun Du: Methodology (equal). Bo Liu: Methodology (equal); Formal analysis (equal); Investigation (equal); Writing – original draft (equal). Yu Yan: Methodology (equal). Liang He: Methodology (equal). Jing Wu: Methodology (equal). Rong Zhang: Conceptualization (equal); Methodology (equal). Bo Liu: Methodology (equal). Tiejun Zhou: Methodology (equal). Yongbing Xu: Data curation (equal); Formal analysis (equal); Funding acquisition (equal); Methodology (equal); Project administration (equal); Supervision (equal); Writing – review & editing (equal). Xuezhong Ruan: Data curation (equal); Formal analysis (equal); Funding acquisition (equal); Methodology (equal); Project administration (equal); Supervision (lead); Writing – review & editing (lead).

DATA AVAILABILITY

The data that support the findings of this study are available from the corresponding author upon reasonable request.

REFERENCES

1 S. Bhatti, R. Sbiaa, A. Hirohata, H. Ohno, S. Fukami, and S.N. Piramanayagam, “Spintronics based random access memory: a review,” Mater. Today 20(9), 530–548 (2017).

2 W. Liu, P.K.J. Wong, and Y. Xu, “Hybrid spintronic materials: Growth, structure and properties,” Prog. Mater. Sci. 99, 27–105 (2019).

3 P. Cappelletti, and J. Slaughter, “6 - Embedded memory solutions: Charge storage based, resistive and magnetic,” in Semicond. Mem. Syst., edited by A. Redaelli and F. Pellizzer, (Woodhead Publishing, 2022), pp. 159–215.

4 J. Hayakawa, S. Ikeda, Y.M. Lee, F. Matsukura, and H. Ohno, “Effect of high annealing temperature on giant tunnel magnetoresistance ratio of CoFeB/MgO/CoFeB magnetic tunnel junctions,” Appl. Phys. Lett. 89(23), 232510 (2006).

5 S. Mangin, D. Ravelosona, J.A. Katine, M.J. Carey, B.D. Terris, and E.E. Fullerton, “Current-induced magnetization reversal in nanopillars with perpendicular anisotropy,” Nat. Mater. 5(3), 210–215 (2006).

6 V. Baltz, A. Manchon, M. Tsoi, T. Moriyama, T. Ono, and Y. Tserkovnyak, “Antiferromagnetic spintronics,” Rev. Mod. Phys. 90(1), 015005 (2018).

7 A. Dal Din, O.J. Amin, P. Wadley, and K.W. Edmonds, “Antiferromagnetic spintronics and beyond,” Npj Spintron. 2(1), 25 (2024).

8 M.B. Jungfleisch, “Perspectives of antiferromagnetic spintronics,” Phys. Lett. A 382, 865–871 (2018).

9 H. Chen, L. Liu, X. Zhou, Z. Meng, X. Wang, Z. Duan, G. Zhao, H. Yan, P. Qin, and Z. Liu, “Emerging Antiferromagnets for Spintronics,” Adv. Mater. 36(14), 2310379 (2024).

10 D. Xiong, Y. Jiang, K. Shi, A. Du, Y. Yao, Z. Guo, D. Zhu, K. Cao, S. Peng, W. Cai, D. Zhu, and W. Zhao, “Antiferromagnetic spintronics: An overview and outlook,” Fundam. Res. 2(4), 522–534 (2022).

11 J. Guo, X. Zhao, Z. Lu, P. Shi, Y. Tian, Y. Chen, S. Yan, L. Bai, and M. Harder, “High exchange-bias blocking temperature in an ultrathin amorphous antiferromagnet system,” Phys. Rev. B 104(10), L100401 (2021).

12.	van der Zaag, P. J. et al. Difference between Blocking and Néel Temperatures in the Exchange Biased Fe3O4/CoO System. Phys. Rev. Lett. 84, 6102–6105 (2000).

13 S. Couet, K. Schlage, R. Rüffer, S. Stankov, Th. Diederich, B. Laenens, and R. Röhlsberger, “Stabilization of Antiferromagnetic Order in FeO Nanolayers,” Phys. Rev. Lett. 103(9), 097201 (2009).

14. B.-Y. Wang, F..-T Lin, Y. -C, Huang, F.-Y. Li, C. -H. Chen, K, -H. Lu, B. -X. Liao, “Perpendicular magnetic anisotropy induced by antiferromagnetic FexMn1-xalloy films: Influence of antiferromagnetic spin structure and long-range ordering.” Phys. Rev. B 109, 214416 (2024).

15 B.-Y. Wang, J.-Y. Ning, T.-H. Li, C.-C. Chung, C.-Y. Hsu, M.-S. Tsai, T.-H. Chuang, and D.-H. Wei, “Antiferromagnet-induced perpendicular magnetic anisotropy in ferromagnetic Co/Fe films with strong in-plane magnetic anisotropy,” Phys. Rev. B 105(18), 184415 (2022).

16 B.-Y. Wang, J.-Y. Lee, W.-L. Li, K. Lin, M.-S. Tsai, T.-H. Chuang, and D.-H. Wei, “Perpendicular magnetic anisotropy induced by antiferromagnetic Mn-Pd alloy films: Dual effects of exchange and spin-orbit coupling,” Phys. Rev. B 107(10), 104429 (2023).

17 B.-Y. Wang, B.-X. Liao, H.-H. Chen, and K.-H. Lu, “Enhanced antiferromagnet-induced perpendicular magnetic anisotropy by Bi atomic layer with high spin–orbit coupling,” Appl. Phys. Lett. 126(15), 152406 (2025).

18 K. Lenz, S. Zander, and W. Kuch, “Magnetic Proximity Effects in Antiferromagnet/Ferromagnet Bilayers: The Impact on the Néel Temperature,” Phys. Rev. Lett. 98(23), 237201 (2007).

19 X. Wu, H. Wang, H. Liu, Y. Wang, X. Chen, P. Chen, P. Li, X. Han, J. Miao, H. Yu, C. Wan, J. Zhao, and S. Chen, “Antiferromagnetic–Ferromagnetic Heterostructure‐Based Field‐Free Terahertz Emitters,” Adv. Mater. 34(42), 2204373 (2022).

20 Y. Fan, X. Ma, F. Fang, J. Zhu, Q. Li, T.P. Ma, Y.Z. Wu, Z.H. Chen, H.B. Zhao, and G. Lupke, “Photoinduced spin angular momentum transfer into an antiferromagnetic insulator,” Phys. Rev. B 10(5), 054037 (2014).

21 W. Zhang, Q. Liu, Z. Yuan, K. Xia, W. He, Q. Zhan, X. Zhang, and Z. Cheng, “Enhancement of ultrafast demagnetization rate and Gilbert damping driven by femtosecond laser-induced spin currents in Fe81Ga19/Ir20Mn80 bilayers,” Phys. Rev. B 100(10), 104412 (2019).

22 L. Frangou, S. Oyarzún, S. Auffret, L. Vila, S. Gambarelli, and V. Baltz, “Enhanced Spin Pumping Efficiency in Antiferromagnetic IrMn Thin Films around the Magnetic Phase Transition,” Phys. Rev. Lett. 116(7), 077203 (2016).

23 Y. Liu, Z. Ji, Y. Zhang, Y. Song, G. Wu, S. Lou, Z. Zhang, and Q. Jin, “Gilbert Damping Modulated by the Exchange Spring Effect in IrMn/CoFe Bilayers,” ACS Appl. Electron. Mater. 5(5), 2732–2737 (2023).

24 S.P. Bommanaboyena, D. Backes, L.S.I. Veiga, S.S. Dhesi, Y.R. Niu, B. Sarpi, T. Denneulin, A. Kovács, T. Mashoff, O. Gomonay, J. Sinova, K. Everschor-Sitte, D. Schönke, R.M. Reeve, M. Kläui, H.-J. Elmers, and M. Jourdan, “Readout of an antiferromagnetic spintronics system by strong exchange coupling of Mn2Au and Permalloy,” Nat. Commun. 12, 6539 (2021).

25 M. Jourdan, H. Bräuning, A. Sapozhnik, H.-J. Elmers, H. Zabel, and M. Kläui, “Epitaxial Mn2Au thin films for antiferromagnetic spintronics,” J. Phys. Appl. Phys. 48(38), 385001 (2015).

26 V.M.T.S. Barthem, C.V. Colin, H. Mayaffre, M.-H. Julien, and D. Givord, “Revealing the properties of Mn2Au for antiferromagnetic spintronics,” Nat. Commun. 4(1), 2892 (2013).

27 H.-C. Wu, Z.-M. Liao, R.G.S. Sofin, G. Feng, X.-M. Ma, A.B. Shick, O.N. Mryasov, and I.V. Shvets, “Mn2Au: Body-Centered-Tetragonal Bimetallic Antiferromagnets Grown by Molecular Beam Epitaxy,” Adv. Mater. 24(47), 6374–6379 (2012).

28 R. Zhang, and R.F. Willis, “Thickness-Dependent Curie Temperatures of Ultrathin Magnetic Films: Effect of the Range of Spin-Spin Interactions,” Phys. Rev. Lett. 86(12), 2665–2668 (2001).

29 F. Shahzad, K. Nadeem, J. Weber, H. Krenn, and P. Knoll, “Magnetic behavior of NiO nanoparticles determined by SQUID magnetometry,” Mater. Res. Express 4(8), 086102 (2017).

30 T. Liu, Y. Zhang, J.W. Cai, and H.Y. Pan, “Thermally robust Mo/CoFeB/MgO trilayers with strong perpendicular magnetic anisotropy,” Sci. Rep. 4(1), 5895 (2014).

31 B. Liu, L. Yang, X. Ruan, J.-W. Cai, L. He, H. Meng, J. Wu, and Y. Xu, “Femtosecond laser-heating effect on the magnetization dynamics in perpendicularly magnetized Ta/CoFeB/MgO film,” New J. Phys. 21(5), 053032 (2019).

32 B. Liu, X. Ruan, Z. Wu, H. Tu, J. Du, J. Wu, X. Lu, L. He, R. Zhang, and Y. Xu, “Transient enhancement of magnetization damping in CoFeB film via pulsed laser excitation,” Appl. Phys. Lett. 109(4), 042401 (2016).

33 T. Liu, Y. Zhang, J.W. Cai, and H.Y. Pan, “Thermally robust Mo/CoFeB/MgO trilayers with strong perpendicular magnetic anisotropy,” Sci. Rep. 4(1), 5895 (2014).

34 F. Offi, W. Kuch, and J. Kirschner, “Structural and magnetic properties of FexMn1-x thin films on Cu(001) and on Co/Cu(001),” Phys. Rev. B 66(6), 064419 (2002).

35 D. Huang, X. Wang, and D.B. Gopman, “Acceleration of ferromagnetic resonance measurements by Bayesian experimental design,” Rev. Sci. Instrum. 95(10), 103906 (2024).

36 W. Stoecklein, S.S.P. Parkin, and J.C. Scott, “Ferromagnetic resonance studies of exchange-biased Permalloy thin films,” Phys. Rev. B 38(10), 6847–6854 (1988).

37 J. McCord, R. Kaltofen, T. Gemming, R. Hühne, and L. Schultz, “Aspects of static and dynamic magnetic anisotropy in Ni81Fe19-NiO films,” Phys. Rev. B 75(13), 134418 (2007).

38 J. Geshev, L.G. Pereira, and J.E. Schmidt, “Rotatable anisotropy and coercivity in exchange-bias bilayers,” Phys. Rev. B 66(13), 134432 (2002).

39 J. McCord, R. Mattheis, and D. Elefant, “Dynamic magnetic anisotropy at the onset of exchange bias: The NiFe/IrMn ferromagnet/antiferromagnet system,” Phys. Rev. B 70(9), 094420 (2004).

40 O. Gladii, L. Frangou, G. Forestier, R.L. Seeger, S. Auffret, I. Joumard, M. Rubio-Roy, S. Gambarelli, and V. Baltz, “Unraveling the influence of electronic and magnonic spin-current injection near the magnetic ordering transition of IrMn metallic antiferromagnets,” Phys. Rev. B 98(9), 094422 (2018).

41 R. Xiong, B. Fang, G. Li, Y. Xiao, M. Tang, and Z. Li, “Electric-field tuning of ferromagnetic resonance in CoFeB/MgO magnetic tunnel junction on a piezoelectric PMN-PT substrate,” Appl. Phys. Lett. 111(6), 062401 (2017).

42 B. Khodadadi, J.B. Mohammadi, C. Mewes, T. Mewes, M. Manno, C. Leighton, and C.W. Miller, “Enhanced spin pumping near a magnetic ordering transition,” Phys. Rev. B 96(5), 054436 (2017).

43 S. Sampan-a-pai, J. Chureemart, R.W. Chantrell, R. Chepulskyy, S. Wang, D. Apalkov, R.F.L. Evans, and P. Chureemart, “Temperature and Thickness Dependence of Statistical Fluctuations of the Gilbert Damping in Co-Fe-B/MgO Bilayers,” Phys. Rev. Appl. 11(4), 044001 (2019).

44 R. Arias, and D.L. Mills, “Extrinsic contributions to the ferromagnetic resonance response of ultrathin films,” Phys. Rev. B 60(10), 7395–7409 (1999).

45 S. Hu, E. Liu, Y. Bai, M. Zhuang, W. Liu, M. Lei, Y. Zhang, G. Xu, F. Xu, and S. Mangin, “Strain-enhanced spin-orbit coupling in permalloy thin films,” Phys. Rev. B 109(22), 224407 (2024).

46 S.N. Panda, S. Mondal, J. Sinha, S. Choudhury, and A. Barman, “All-optical detection of interfacial spin transparency from spin pumping in β-Ta/CoFeB thin films,” Sci. Adv. 5(4), eaav7200 (2019).

47 Y. Gong, X. Lu, and J. Su, “Tuning interfacial spin pump in Ta/CoFeB/MgO films by ultrafast laser pulse,” Appl. Phys. Lett. 119, 092404 (2021).

48 Z. Zhu, S. Chen, B. Zhao, Q.Y. Jin, J. Chen, and Z. Zhang, “Control of perpendicular magnetic anisotropy and spin pumping damping in MgO/CoFeB/Ta/Pt structures,” J. Phys. Appl. Phys. 50(35), 355001 (2017).

49 J.M. Lommel, and C.D. Graham Jr., “Rotatable Anisotropy in Composite Films,” J. Appl. Phys. 33(3), 1160–1161 (1962).

50 T. Chatterji, and G.J. McIntyre, “Antiferromagnetic phase transition and spin correlations in NiO,” Phys. Rev. B 79, 172403 (2009).

51 Z. Qiu, J. Li, D. Hou, E. Arenholz, A.T. N’Diaye, A. Tan, K. Uchida, K. Sato, S. Okamoto, Y. Tserkovnyak, Z.Q. Qiu, and E. Saitoh, “Spin-current probe for phase transition in an insulator,” Nat. Commun. 7(1), 12670 (2016).

52 W. Lin, K. Chen, S. Zhang, and C.L. Chien, “Enhancement of Thermally Injected Spin Current through an Antiferromagnetic Insulator,” Phys. Rev. Lett. 116(18), 186601 (2016).

53 F. Basheer Abdulahad, D.-S. Hung, and S.-F. Lee, “Temperature dependence of static and dynamic magnetic properties in NiFe/IrMn bilayer system,” J. Mater. Res. 29(11), 1237–1247 (2014).

54 O. Gladii, L. Frangou, G. Forestier, R.L. Seeger, S. Auffret, M. Rubio-Roy, R. Weil, A. Mougin, C. Gomez, W. Jahjah, J.-P. Jay, D. Dekadjevi, D. Spenato, S. Gambarelli, and V. Baltz, “Spin pumping as a generic probe for linear spin fluctuations: demonstration with ferromagnetic and antiferromagnetic orders, metallic and insulating electrical states,” Appl. Phys. Express 12(2), 023001 (2019).

55 M. Dąbrowski, T. Nakano, D.M. Burn, A. Frisk, D.G. Newman, C. Klewe, Q. Li, M. Yang, P. Shafer, E. Arenholz, T. Hesjedal, G. van der Laan, Z.Q. Qiu, and R.J. Hicken, “Coherent Transfer of Spin Angular Momentum by Evanescent Spin Waves within Antiferromagnetic NiO,” Phys. Rev. Lett. 124(21), 217201 (2020).

56 A.B. Shick, S. Khmelevskyi, O.N. Mryasov, J. Wunderlich, and T. Jungwirth, “Spin-orbit coupling induced anisotropy effects in bimetallic antiferromagnets: A route towards antiferromagnetic spintronics,” Phys. Rev. B 81(21), 212409 (2010).

57 Z. Zhu, G. Wu, Y. Ren, S. Lou, Q.Y. Jin, and Z. Zhang, “Modulation of magnetic damping in antiferromagnet/CoFeB heterostructures,” Appl. Phys. Lett. 116(18), 182407 (2020).

58 H. Saglam, W. Zhang, M.B. Jungfleisch, J. Sklenar, J.E. Pearson, J.B. Ketterson, and A. Hoffmann, “Spin transport through the metallic antiferromagnet FeMn,” Phys. Rev. B 94(14), 140412 (2016).

59 H. Bai, W. Zhu, Y. You, X. Chen, X. Zhou, F. Pan, and C. Song, “Size-dependent anomalous Hall effect in noncollinear antiferromagnetic Mn3Sn films,” Appl. Phys. Lett. 117(5), 052404 (2020).

60 K. Akin, H. Piskin, E. Selvi, E. Demircanli, S. Ari, M.H. Ramezan zadeh, B. Kocaman, and O. Ozatay, “Correlation of blocking and Néel temperatures in ultrathin metallic antiferromagnets,” Phys. Rev. Appl. 22(4), 044037 (2024).