## Slide 1: Sustainability Challenges of the Textile & Dyeing Industries – opportunities for innovation
Centre for Technical Textiles
SUSTAINABLE MATERIALS RESEARCH GROUP
Dr. Richard Blackburn
Sustainable Materials Research Group
University of Leeds
@RichardBlackb18

## Slide 2: Necessity for Sustainable Products
2012 - world population 7 billion
2050 - expected to rise to over 9 billion
Increases demand
      food, energy, water, resources, chemicals
Increases environmental burden
      pollution
      depletion of finite non-renewable resources (e.g. fossil fuels)
Synthetic chemical products and processes afford a significant improvement in quality of life
Growing middle class want these consumer products too

## Slide 3: Synthetic fibre revolution
20th Century polymers
      nylon, 1935
      polyurethane, 1937
      polyester
        Terylene, 1941
        Dacron, 1946
      acrylic, 1944
      polypropylene and HDPE,1951
Notes: Many new polymers invented in 20th Century
  Wallace Carothers and DuPont: nylon, 1935
  Bayer: polyurethane, 1937
  Whinfield, Dickson, Birtwhistle and Ritchie (ICI): first polyester fibre (Terylene), 1941
  DuPont: acrylic, 1944
  DuPont: Dacron (polyester), 1946
  Banks and Hogan: polypropylene and high density polyethylene, 1951
Non-degradable and non-renewable
Their use increases oil consumption significantly
Polyester now has the highest consumption of all fibres
At the current rate of consumption, fossil fuels expected to last for another 50-60 years

## Slide 4: Synthetic fibre sustainability challenges
Non-degradable
Non-renewable
Increases oil consumption
Contribution to anthropogenic GHGs
Significant oil supply issues
But, polyester highest share of textile market (>50m tpa)
Raw materials for fibres must change
Recyclable – mechanical or chemical?
Notes: Many new polymers invented in 20th Century
  Wallace Carothers and DuPont: nylon, 1935
  Bayer: polyurethane, 1937
  Whinfield, Dickson, Birtwhistle and Ritchie (ICI): first polyester fibre (Terylene), 1941
  DuPont: acrylic, 1944
  DuPont: Dacron (polyester), 1946
  Banks and Hogan: polypropylene and high density polyethylene, 1951
Non-degradable and non-renewable
Their use increases oil consumption significantly
Polyester now has the highest consumption of all fibres
At the current rate of consumption, fossil fuels expected to last for another 50-60 years

## Slide 5: Definition of Sustainability
E
N
V
I
R
O
N
M
E
N
T
S
O
C
I
E
T
Y
E
C
O
N
O
M
Y
Notes: 5

## Slide 6: Sustainability considerations
WATER
EMISSIONS
ENERGY
RAW MATERIALS
Notes: 6

## Slide 7: Public perception
Demand (and rejection) for consumer products can be driven by the public and the media
“Biodegradable”, “Natural”, “Organic”
      perceived by the public to be good for the environment
“Synthetic”, “Non-organic”, “GM”
      perceived by the public to be bad for the environment
“Chemistry”
      Public perception of science…
Do the public understand what “Sustainable” means?
Physics
Chemistry
Notes: Some industries use this to their advantage
Something purported as ‘green’ is often not so in reality

## Slide 8: Ideal sustainable product
  Provide an equivalent function to the product it replaces
  Performs as well as or better than the existing product
  Be available at a competitive or lower price
  Have a minimum environmental footprint for all the processes involved
  Be manufactured from renewable resources
  Use only ingredients that are safe to both humans and the environment
  No negative impact on food supply or water

## Slide 9: RØADMAP TO ZERO DISCHARGE OF HAZARDOUS CHEMICALS (ZDHC)
Has involved stakeholders in development
Provides training to industry
Looks at hazards in the manufacturing supply chain, not just final products
      Tests final textile products
      But in the manufacturing supply chain it is largely based on a chemical inventory approach (overlooks impurities and by-products in chemical used)

## Slide 10: RØADMAP TO ZERO DISCHARGE OF HAZARDOUS CHEMICALS (ZDHC)
Does not actually eliminate substances of concern to zero concentrations, but restricts to a limit of n ppm
Does not cover a wide range of chemicals on its MRSL
Only chemicals with very low limits are PFOA and PFOS at 2 ppm
Is the focus on these chemistries influenced by Greenpeace (Chemistry for any weather, October 2012)?
Creditable to reduce levels of PFOA and PFOS, but there is more concerning chemistry issues in the textile industry

## Slide 11: Textile dyeing processes
Traditional dyeing processes use 5.8 trillion litres water p.a.
      ~3.7 billion Olympic swimming pools
10-20% dye remains after dyeing (plus other chemicals), leaving potential for wastewater pollution
      One fifth of the world's industrial water pollution (World Bank)
391 billion kWh energy for dyeing processes
Innovative technologies needed to reduce, or eliminate, water, energy and auxiliary chemicals in dyeing

## Slide 12: Treatment of textile dyeing effluent
Wastewater discharged from dyeing processes one of biggest contributors to textile effluent
Mainly residual dyes and auxiliary chemicals
>50,000 tpa dye discharged into effluent
Dye Class | Fibre | Loss to effluent (% applied)
acid | polyamide | 5-20
basic | acrylic | 0-5
direct | cotton | 5-30
disperse | polyester | 0-10
metal-complex | wool/polyamide | 2-10
reactive | cotton | 10-50
sulfur | cotton | 10-40
vat | cotton | 5-20

## Slide 13: Treatment of textile dyeing effluent
Dyeing effluent in a watercourse aesthetically undesirable, but has a more serious environmental impact
High BOD combined with spectral absorption of dye
      Can affect photosynthetic processes
      Reduction in O2 levels in the water → suffocation of aquatic flora and fauna
Dyestuffs may be also have aquatic toxicity (metals, AOX)
Several methods developed to remove colour from dyehouse effluent
Varying in effectiveness, economic cost, and environmental impact (of the treatment process itself)
Blackburn RS, Environ. Sci. Technol. 2004, 38, 4905.

## Slide 14: Polyester dyeing process
Hydrophobic fibre dyed with hydrophobic disperse dye
Traditional aqueous process requires dispersing agents/surfactants and high temperatures (typically 130 °C) under pressure
Other dyeing auxiliaries often required
Large amount of waste dye left over in effluent
Surface dye removed with surfactants and/or reducing agents
Innovation in scCO2 dyeing to completely change polyester dyeing process

## Slide 15: scCO2 dyeing - timeline
1988
Schollmeyer et al. patent scCO2 dyeing of polyester
Process further developed by Knittel et al.
1992
1995
Pilot scale dyeing of polyester up to 30 L (Bach et al.)
Dyeing of modified cotton in scCO2 at Univ of Leeds
1998
2010
DyeCoo deliver first industrial-scale scCO2 dyeing machine to factory in Thailand
Abel Kirui wins silver in London 2012 Marathon singlet in dyed using DyeCoo process
2012
2013
Nike opens dedicated waterless dyeing factory in Taiwan

## Slide 16: scCO2 dyeing
START
Fabric loaded
STEP 1
Liquid CO2 released into dyeing vessel
STEP 2
Heat + pressure liquid CO2 → scCO2
STEP 3
scCO2 and dye forced through fibre
STEP 4
Fresh CO2 pumped through and used CO2 to separator
STEP 5
Separator evaporates CO2 to remove excess dye and residue
STEP 6
Pressure lowered and CO2 leaves vessel as gas. 95% recovered
FINISH
Dyed fabric

## Slide 17: scCO2 dyeing
System comparison with traditional polyester dyeing
WATER
Zero water used
WASTEWATER
Nearly 100% dye used in process.
Zero waste
PROCESS CHEMICALS
No auxiliary chemicals required
FOOTPRINT
¼ of physical footprint to dye same amount of fabric
EFFICIENCY
40% faster than traditional dyeing processes
ENERGY
Reduces energy consumption by 63%

## Slide 18: scCO2 dyeing - limitations
Machines are more expensive than traditional water-dyeing machines
      “costs will come down through scale and lower water and energy expenses“
Only works on polyester fabrics and can't be used to dye cotton
      Cotton made up about 32% global fibre market in 2012
      Some relatively unsuccessful work on modifying cotton
Significant opportunity to develop low or zero water dyeing systems for coloration of cellulosics

## Slide 19: Coloration of cotton
Dyeing of cotton primarily conducted using reactive dyes
Despite development of dyes with high fixation, dyeing still uses high quantities of salt, water (and energy), and creates colour pollution
Soil too alkaline to support crops
Kills aquatic life
Fresh watercourses turned saline downstream from dyehouses
Difficult to remove from effluent
  10-40% dyestuff hydrolysed
    Goes down drain
    Aesthetically unpleasant
    Blocks sunlight
      Kills aquatic life
Clean effluent
    High cost
  High level in dyeing
  Incredible volume in wash-off
    Up to 10 separate rinsings
      High energy consumption
      50% total cost dyeing procedure

## Slide 20: Wash-off of reactive dyeings on cotton
      Dye transfer inhibiting (DTI) polymers (used in laundry detergents) were employed to remove unfixed dyes
      Much more efficient, economical and sustainable process developed
      Significantly reduces operation time, water consumption and energy consumption
          poly(vinylpyridine-N-oxide) polymers were the most effective
          poly(vinylpyridine betaine) polymers also highly efficient
Procedure | Time (min) | Water (L/kg fabric) | Energy (MJ/kg fabric)
recommended wash-off | 250 | 60 | 9.21
DTI wash-off | 50 | 30 | 0.84
Amin MN, Blackburn RS, ACS Sus. Chem. Eng. 2015, 3, 725.

## Slide 21: Bigger problems with cotton
NATURAL doesn’t necessarily mean sustainable
Cotton production >25 million tpa
High levels of pesticides (25% world total)
High levels of insecticides (11% world total)
Very high irrigation levels
      1 kg of cotton fibre requires 20,000-40,000 L
      Water average person consumes in a lifetime
Only grows in certain climates
      Deforestation to grow cotton
High area of land for mass of useable fibre

## Slide 22: Sustainable cotton?
Organic cotton
Widely promoted as the answer to cotton’s problems
Global production (in over 20 countries, mainly India) only 1.1% of world cotton production
No genetically modified seed permitted
No herbicides or pesticides
Ethical labour employment standards
Requires approximately 1.4x area of land to produce same mass of fibre
Still has very high water consumption
Not a viable alternative on a global scale to completely replace non-organic cotton

## Slide 23: Sustainable cotton?
Better cotton
GM pest-resistant strain referred to as ‘Bt cotton’
      Naturally occurring protein (used by organic gardeners) – kills bollworm pests (moth larva)
      Reduces pesticide sprays from 5 sprays to 0
      Poisoning of workers virtually eliminated
      More productive, particularly in India
      Bt cotton is regarded as less ‘natural’
      Cannot be classed as ‘organic’
Better Cotton Initiative (BCI) set up to foster improvements in the sustainability of cotton production methods

## Slide 24: Sustainable Cellulosic Fibres
Bast Fibres
        From stem of plants (flax, hemp, jute, ramie, nettle, kenaf, abaca)
        Plants with opportunities for performance fibres (e.g. Himalayan nettle)
        Processing to separate ultimate fibres is of concern
        Opportunities for innovation into alternative separation techniques (e.g. enzyme-assisted technologies)
Blake AW, Marcus SE, Copeland JE, Blackburn RS, Knox JP, Planta, 2008, 228, 1.
Lanzilao G, Goswami P, Blackburn RS, Mater. Letts., 2016, in press.

## Slide 25: TENCEL (lyocell) – most sustainable fibre production process
wood
pulp
Fibre production
Tencel®
Wood from certified forests
Direct dissolution process
N-methylmorpholine-N-oxide (NMMO)
Closed-loop process
>99% recovery of solvent
Regenerated cellulosics made from trees
Lenzing manufactures lyocell

## Slide 26: Green footprint: significantly more environmentally than cotton
More than 50% of Lenzing’s fuel consumption sourced from renewable resource

## Slide 27: Sustainability challenges for the textiles industry
Sustainability issues in the textiles industry have often been tackled in industry by tinkering and incremental change
Step-change solutions are needed to bring about truly sustainable apparel and footwear products

## Slide 28: Best way to mix colours?
Nano-level
      Mixture of different dye molecules in dyebath to create desired shade
Micro-level
      Mixture of different dyed fibres in yarn formation process to create desired shade

## Slide 29: Does fibre coloration have to be through dyeing?
Dope-dyeing: incorporation of colorant into spinning process
Lyocell process makes this possible for cellulosics
Cellulose pulp
Dyeing pulp
Mixing dyed pulp with undyed pulp
Dissolution in NMMO
Fibre spinning and washing
Dope-dyed lyocell fibres

## Slide 30: DyeCat Process
Catalytic process that allows colour to be integrated directly into polyesters
Eliminates need for conventional dyeing
Colour in fibre is generated at the same time the polymer is made
Colours ‘locked into’ fibre providing a technically superior product
No need for wasteful dyeing processes
DyeCat PLA fibre
      Renewable
      Technically superior
      Saves chemicals and energy

## Slide 31: DyeCat Process
Coloration of polymer during synthesis
Demonstrated on PLA using coloured catalysts
MacRae RO, Pask CM, Burdsall LK, Blackburn RS, Rayner CM, McGowan PC, Angew. Chem. Int. Ed. 2010, 50, 291.

## Slide 32: Novel, sustainable and cost-effective textile dyeing using nanocellulosic fibres
Dr. Yunsang Kim et al., University of Georgia
Innovative dyeing processes using coloured nanocellulose
Winner of Green and Sustainable Chemistry Challenge
nano-sized cellulose fibrils (wood pulp) + dye
    → dyed nanocellulose dispersion
Apply dyed nanocellulose dispersion onto the textile material using low water process
    Coloured nanocellulose permanently binds to textile surface
    Greatly reduces energy and water needed

## Slide 33: Fast Fashion
Consumption of new designs as close as possible to the point of creation
Fast, low price and disposable
Business model: reducing time cycles from production to consumption
"Supermarket" market
Environmental Impact
      US imports >1 billion garments annually from China alone
      Dramatic increase in environmental damage caused by the textile industry
      Safety compromised in evermore cost-cutting supply chain
      Human disasters (e.g. Rana Plaza)
An enormous change is needed in the minds and attitudes of retailers and consumers
7m tonnes clothing thrown away in UK every 10 minutes

## Slide 34: Sustainable Urban Living – Textiles
Greater use of sustainable raw materials
Lower energy & water consumption and pollution generation in production
Lower impact in use
      Water, energy, chemicals in cleaning/laundering
Design for easy disassembly/disposal/ recycling
DESIGN FOR REDUCED CONSUMPTION AND LONGER LIFE
    ‘Disposable’ products unsustainable

## Slide 35: Dr. Richard S. Blackburn r.s.blackburn@leeds.ac.uk @RichardBlackb18
Centre for Technical Textiles
SUSTAINABLE MATERIALS RESEARCH GROUP
Thank you